Spring

Helical Torsion Springs

The bending stress can be obtained by using curved-beam theory as explained. It is convenient to write the expression in the form

σ= KMcI

Where K is a stress concentration factor.

Ki=4C2−C−14C(C−1) , Ko =4C2+C−14C(C+1)

We designate D as the mean spring diameter and d as the wire diameter .

Where C is the spring index and subscripts i and o refer to the inner and outer fibers. C = D/d , respectively , The Ko  is less than unity , we shell use only Ki  to determine stresses . When the bending moment M = Fr and section moudulus I/C = πd332 , We obtain

σ= Ki32Frπd3

Which gives the bending stress for a round wire torsion spring.

Deflection

The stain energy in bending is U ,

U=M2dx2EI

For the torsion spring , M=Fr , The force F will deflect through the distance rθ, where θ is the total angular deflection of the sprig. Applying Castigliano’s theorem .

rθ=∂U∂F=0πDNF2r2dx2EI=0πDNFr2dxEI

I= πd464

θ=64FrDNd4E

The spring rate is therefore

k=Frθ=d4E64DN

The spring rate may also be expressed as the torque required to wind up the spring one turn. This is obtained by multiplying by 2π. Thus

k'=d4E10.2DN

Actual tests show that the constant 10.2 should be increased slightly. Thus the equation

k'=d4E10.2DN Will give better results

The endurance limit for torsion springs can be found in a similar manner by using the value of Sse is

Se=kakbkcSe'=78.0 kpsi =(537 Mpa)

The table below provides some typical values for the above variables.

| Material | Diameter Range(mm) | Exponent m | A (MPa) |
| --- | --- | --- | --- |
| Music Wire | 0.1 to 6.5 | 0.145 | 2211 |
| Oil-Tempered | 0.5 to 12 | 0.187 | 1855 |
| Hard Drawn | 0.7 to 12 | 0.190 | 1783 |
| Chrome Vanadium | 0.8 to 12 | 0.168 | 2005 |
| Chrome Silicon | 1.6 to 10. | 0.108 | 1975 |
| 302-Stainless | 0.3 to 2.5. | 0.146 | 1867 |
| 302-Stainless | 2.5 to 5 | 0.263 | 2065 |
| 302-Stainless | 5 to 10 | 0.478 | 2911 |
| Phos-Bros | 0.1 to 0.6 | 0 | 1000 |
| Phos-Bros | 0.6 to 2.0 | 0.028 | 913 |
| Phos-Bros | 2.0 to 7.5 | 0.064 | 932 |

Table 1 .

Spring materials may be compared by an examination of their tensile strengths; these vary so much with wire size that they cannot be specified until the wire size is known. The material and its processing also, of course, have an effect on tensile strength. It turns out that the graph of tensile strength versus wire diameter is almost a straight line for some materials when plotted on log – long paper .Writing the equation of this line as

Sut=Adm

Furnishes a good means of estimating minimum tensile strengths when the intercept A and the slope m of the line are known . Values of these constants have been worked out from recent data and are givens for strengths in units Mpa in Table 1.

In calculating the spring parameters the torsional yield strength (S sy ) is used.   The relationship between the torsional yield strength and the ultimate strength Sut can be approximated with a range as follows.

0,35 Sut =< S sy =< 0,52 Sut

0.78 Sut  cold-drawn carbon steel . (D/d>4 or d<1/4”)

Sy=σall= 0.87 Sut  hardened and tempered carbon and low- alloy steel . (D/d < 4 or d>1/4”)

0.61 Sut  austenitic stainless steel and nonferrous alloys .

材質: 各種合金鋼線ˋ不繡鋼線ˋ高碳鋼線ˋ磷銅線。

產品敘述: 由單扭至雙扭以及各種扭桿之形狀依設計成型，採用自動CNC多軸電腦成型機械加工，適用於各種扭力功能零件使用。

| 種類 | 規格號碼 (日本工業規格) | 記號 | 用途(參考) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 一般用 | 導電 | 非磁 | 耐熱 | 耐蝕 | 耐疲勞 |
| 硬鋼線 | JIS G 3521 | SW(1) | ○ |  |  |  |  |  |
| 鋼琴線 | JIS G 3522 | SWP | ○ |  |  |  |  | ○ |
| 彈簧用油回火碳鋼線 | JIS G 3560 | SWO | ○ |  |  |  |  |  |
| 閥用油回火碳鋼線 | JIS G 3561 | SWO-V |  |  |  |  |  | ○ |
| 閥用油回火鉻釩鋼線 | JIS G 3565 | SWOCV-V |  |  |  | ○ |  | ○ |
| 閥用油回火矽鉻鋼線 | JIS G 3566 | SWOSC-V |  |  |  | ○ |  | ○ |
| 彈簧用油回火矽錳鋼線 | JSMA NO.5 | SWOSM(2) | ○ |  |  |  |  |  |
| 彈簧用不銹鋼線 | IS G 4314 | SUS 302 | ○ |  |  | ○ | ○ |  |
|  |  | SUS 304 | ○ |  |  | ○ | ○ |  |

Fatigue Loading

For helical springs, The worst condition , would occur when there is no preload , that is , when τmin=0 .

So , we define

Fa=Fmax−Fmin2

Fm=Fmax+Fmin2

Use Goodman analysis

When SaSe+SmSut=1 => Mmax(Fr)=πd316ki∗[Se∗SutSe+Sut]

Stress in helical springs

The maximum stress in the wire may be computed by superposition with the cut portion would exert a direct shear force F and a torsion T on the remain part of the spring.

Fig left is Axially loaded helical spring ; right is free body diagram showing that the wire is subjected to a direct shear and a torsional shear .

τmax=±TrJ+FA

Where the term TrJ is the torsion formula and FA is the direct (not flexural) shear stress. Replacing the terms by T=FD2 , r=d2,J=πd432, A=πd24

τ=8FDπd3+4Fπd2

Now we define the spring index

C=Dd

τ=Ks8FDπd3 , Ks=1+12C , Ks is a shear –stress correction factor .

KB=4C+24C−3 , 	This is called the Bergstrasser factor .

Kc=kBks

When fatigue failure is likely or when the spring material must be considered as a brittle material , Kc is treated as a stress-concentration factor and used according to earlier recommendations .

Deflection of helical springs

k=Fy , δ=FlAE

k=AEl

θ=TlGJ

k=Tθ=GJl

U=F2l2AE ------ Tension and compression

U=T2l2GJ ------- Torsion

When U=Fδ2 , Since the shear strain is γ=δl=τG=FAG

U=F2l2AG  direct shear .

U=T2l2GJ+F2l2AG

Substituting T=FD2 , l=πDNr=d2,J=πd432, A=πd24 results in

U=4F2D3Nd4G+2F2DNd2G

Where N=Na=number of active coils . Then , using Castigliano’s theorem ,

Y=∂U∂F=8FD3Nd4G+4FDNd2G

Since C=D/d , that can be rearranged to yield

y=8FD3Nd4G(1+12C2)≈8FD3Nd4G

The spring rate is k=F/y , and so

k=d4G8D3N